UNDERWRITERS LABORATORIES INC.			     APPLIANCE WIRING MATERIAL
Subj. 758		Section 1		Page 1028	     Issued:  1959-05-01
							          Revised:  2004-04-23

Style 1028		Thermoplastic (PVC) - Insulated Wire for Appliance 
			Hook-Up Use.
______________________________________________________________________________

Rating		105C, 600 volts.
______________________________________________________________________________

Conductor		No. 22-6 AWG, tinned or bare copper.
______________________________________________________________________________

Insulation		Class 43, PVC, No. 22-8 AWG minimum average thickness 
			45 mils, minimum thickness at any point 40 mils; 
			No. 7-6 AWG minimum average thickness 60 mils, minimum 
			at any point 54 mils.
______________________________________________________________________________

Covering		None.
______________________________________________________________________________

Standard		Appliance Wiring Material UL 758.
______________________________________________________________________________

Instructions	Detailed Examination.
to UL			Tensile Strength and Elongation of Insulation.
Representative	Spark Test.
______________________________________________________________________________

UL			(4)  Detailed Examination.
Counter-Check	(4)  Tensile Strength and Elongation of Insulation.
Program		(4)  Heat Shock.
			(4)  Deformation.
			(4)  Cold Bend.
*			(12) Horizontal Flame Test.
______________________________________________________________________________

Marking		General.
______________________________________________________________________________

Use			Internal wiring of appliances where exposed to 
			temperatures not exceeding 105C; or internal wiring 
			of appliances where exposed to temperatures not 
			exceeding 105C, or where exposed to oil at a temperature 
			not exceeding (60C or 80C, whichever is applicable.)

			Tags may indicate the following:  2500 Volts Peak - 
			For Electronic Use Only.