UNDERWRITERS LABORATORIES INC.			     APPLIANCE WIRING MATERIAL
Subj. 758		Section 2		Page 2960	     Issued:  1978-09-28
								    Revised:  2003-03-31

Style 2960		Multi-Conductor Cable.
______________________________________________________________________________

Rating		60C, 30 Volts.
______________________________________________________________________________

Conductors		No. 32 AWG minimum solid or stranded.
______________________________________________________________________________

Insulation 		Polypropylene, or polyethylene wall thickness may vary 
			from 3.5 minimum at any point to 30 mils maximum.
______________________________________________________________________________

Assembly		Consists of two or more conductors, twisted pairs or 
groups of twisted conductors twisted together.  The conductors or groups of conductors may be laid parallel forming a flat, oval or round cable.  The lay of the conductors is not specified.  A barrier layer and/or fillers are optional.  Manufacturer shall maintain a complete description of each assembly.  May use same or mixed AWG size.
______________________________________________________________________________

Covering		(Optional) A 6 mil or heavier PVC covering may be 
			extruded over the conductor assembly.
______________________________________________________________________________

Shielding		Optional.
______________________________________________________________________________

Jacket		PVC - Class 43

					     Thickness of PVC Jacket

			#Dia of Cable      Min. Average     Min. Thickness
			 under Jacket        Thickness       at any point
			  in inches           in mils          in mils    
			                  Constr. Constr.   Constr. Contr.
			                    A       B         A       B  

			0.250 or less       15     30         12     24
			0.251 - 0.425       30     30         24     24
			0.426 - 0.700       45     45         36     36

			# - Major dia if cable is flat or oval.
____________________________________________________________________________
							     	(Continued on Page 2960A)

UNDERWRITERS LABORATORIES INC.			     APPLIANCE WIRING MATERIAL
Subj. 758		Section 2		Page 2960A       Issued:  1978-09-28
							          Revised:  2003-03-31

Standard		Appliance Wiring Material UL 758.
______________________________________________________________________________

Instructions	Detailed Examination.
to UL			Tensile Strength and Elongation of Jacket.
Representative
______________________________________________________________________________

UL			(4)  Detailed Examination.
*Counter-Check	(4)  Physical Properties of Jacket.
Program		(4)  Heat Shock on Jacket.
			(4)  Deformation on Jacket.
			(4)  Cold Bend.
*			(12) Cable Flame Test, Construction B only.
*			(12) Horizontal Flame Test, Construction A only.
______________________________________________________________________________

Marking		General.
______________________________________________________________________________

Use			Construction A

			Internal wiring of electronic equipment (such as 
			computers and electric business machines).

			Construction B

			External interconnection of electronic computers and
			electric business machines.