UNDERWRITERS LABORATORIES INC.			     APPLIANCE WIRING MATERIAL
Subj. 758	   	Section 1		Page 1689        Issued:  April 21, 1976
				           			    Revised:  Feb. 16, 2004

Style 1689		Thermoplastic (ECTFE) Insulated Wire.
______________________________________________________________________________

Rating		105C, No voltage rating.
______________________________________________________________________________

Conductor		No. 30-16 AWG consisting of solid or stranded tinned, 	*	  		silver plated or nickel plated copper.
______________________________________________________________________________

Insulation		10 mils min. avg., 8 mils min. at any point wall of ethylene 
			Chlorotrifluoroethylene resin.
______________________________________________________________________________

*Standard		Appliance Wiring Material UL 758.
______________________________________________________________________________

Instructions	Detailed Examination.
*to UL		Flexing, except using mandrel two times diameter of
Representative	   wire.
*			Spark Test, 2000 Volts.
			Tensile Strength and Elongation, as received, (4500 psi and 
	   		   100 per cent elongation, minimum acceptable values).
______________________________________________________________________________

UL			(4)  Detailed Examination.
Counter-Check	(4)  Age 60 days in air-oven at 113C after which samples
*Program	    	     shall be flexed, except using mandrel two times 					     diameter of wire.
			(4)  Tensile Strength and Elongation, same as above.
*			(12) Horizontal Flame Test.
______________________________________________________________________________
	  
*Marking		General.
______________________________________________________________________________

Use			In office appliances.