# Approval Sheet

for

# Thick Film Chip Resistor

# RC series

±1% & ±5%

# YAGEO CORPORATION

THICK FILM FACTORY

Factory: No.11, Min Chuan Rd., Ta Sheh, Kaohsiung, Taiwan, R.O.C.

Tel: 886-7-351-4117   Fax: 886-7-351-2075

Headquarters: 3F, No.233-1, Pao Chiao Rd., Shin Tien, Taipei, Taiwan, R.O.C.

Tel: 886-2-2917-7555   Fax: 886-2-2917-4286

URL: www.yageo.com.tw

1.  SUBJECT: This specification describes of RC series chip resistors made of YAGEO Corporation by thick film process.

2.  PART NUMBER: Part number of the chip resistor is identified by the series, size, tolerance, packing style, temperature coefficient, special type and resistance value.

Example：

RC     0603       F         R         -          07       10K

Series    Size    Resistance   Packing   Temperature   Special   Resistance

Name    Code    Tolerance     Style   	   Coefficient       Type     	  Value                 			                       	       of Resistance

(1) Size        Chip:  0201  0402  0603  0805  1206

Power Chip:   1210  2010  2512

(2) Tolerance: F=±1%    J=±5%

(3) Packaging Type:	R＝Paper Taping Reel.

C＝Bulk Cassette.

K＝Embossed Taping Reel

(4) T.C.R: E=±50ppm/℃ F=±100ppm/℃ G=±200ppm/℃ — =lgnore

(5) Special Type:   07＝ 7 inch Dia. Reel

10＝10 inch Dia. Reel

13＝13 inch Dia. Reel

(6) Resistance Value: 1R、10R、100R、10K、100K、330K、1M………

- MARKING:

Marking Explanation:

- RC0805/RC1206/ RC1210/RC2010/RC2512

Either resistance in E-24 or E-96 series: 4 digits, first three digits are significant figures, fourth digit is number of zeros.

Value =10KΩ

(2) RC0603/RC0805/RC1206/RC1210/RC2010/RC2512

When resistance in E-24 series: 3 digits, first two digits are significant figures, third digit is number of zeros.

Value =10KΩ

(3) RC0603

When resistance in E-96 series: 3 digits, use 0603 ±1% EIA-96 marking method. When ±1% tol in E-24 series,protective layer distinquished with

blue color

Value =12.4 KΩ

EIA-96 MARKING

| Code R Value | Code R Value | Code R Value | Code R Value | Code R Value | Code R Value | Code R Value | Code R Value |
| --- | --- | --- | --- | --- | --- | --- | --- |
| 01 100 | 13 133 | 25 178 | 37 237 | 49 316 | 61 422 | 73 562 | 85 750 |
| 02 102 | 14 137 | 26 182 | 38 243 | 50 324 | 62 432 | 74 576 | 86 768 |
| 03 105 | 15 140 | 27 187 | 39 249 | 51 332 | 63 442 | 75 590 | 87 787 |
| 04 107 | 16 143 | 28 191 | 40 255 | 52 340 | 64 453 | 76 604 | 88 806 |
| 05 110 | 17 147 | 29 196 | 41 261 | 53 348 | 55 464 | 77 619 | 89 825 |
| 06 113 | 18 150 | 30 200 | 42 267 | 54 357 | 66 475 | 78 634 | 90 845 |
| 07 115 | 19 154 | 31 205 | 43 274 | 55 365 | 67 487 | 79 649 | 91 866 |
| 08 118 | 20 158 | 32 210 | 44 280 | 56 374 | 68 499 | 80 665 | 92 887 |
| 09 121 | 21 162 | 33 215 | 45 287 | 57 383 | 69 511 | 81 681 | 93 909 |
| 10 124 | 22 165 | 34 221 | 46 294 | 58 392 | 70 523 | 82 698 | 94 931 |
| 11 127 | 23 169 | 35 226 | 47 301 | 59 402 | 71 536 | 83 715 | 95 953 |
| 12 130 | 24 174 | 36 232 | 48 309 | 60 412 | 72 549 | 84 732 | 96 976 |

This table shows the first two digits for the three-digit EIA-96 part marking scheme.

The third character is a letter multiplier :

X=10-1  Y=10-2   A=100   B=101   C=10 2   D=10 3   E=10 4   F=10 5

(4) RC0201/0402

RC0201/0402 no marking

0402       0201

4.  POWER RATING

(1) Rated Power at 70℃: RC0402=1/16W  RC0603=1/10W  RC0805=1/8W  RC1206=1/4W

RC1210=1/3W   RC2010=3/4W   RC2512=1W  RC0201=1/20W

(2) Rated Voltage: The DC or AC (rms) continuous working voltage corresponding to the rated power is determined by the following formula:

V＝  √(P X R)

Where V＝ Continuous rated DC or AC (rms) working voltage(V)

P＝ Rated power (W)

R＝ Resistance value (Ω)

5.  ELECTRICAL CHARACTERISTICS

| Type | RC0201 1/20 w | RC0402 1/16 w | RC0603 1/10 w | RC0805 1/8 w |
| --- | --- | --- | --- | --- |
| Operating Temp. Range | －55℃ ~ ＋125℃ |  |
| Maximum Working Voltage | 25V | 50V | 50V | 150V |
| Maximum Overload Voltage | 50V | 100V | 100V | 300V |
| Dielectric Withstanding Voltage | 50V | 100V | 100V | 300V |
| Resistance Range | 10Ω~1MΩ (E-24) Zero Ohm Jumper<0.05Ω | 2Ω~10MΩ(E-24) 100Ω~2.2MΩ(E-96) Zero Ohm Jumper<0.05Ω | 1Ω~22MΩ(E-24) 10Ω~2.2MΩ(E-96) Zero Ohm Jumper<0.05Ω | 1Ω~22MΩ(E-24) 10Ω~2.2MΩ(E-96) Zero Ohm Jumper<0.05Ω |
| Temperature Coefficient | ±200ppm/℃(10Ω~1MΩ) | ±200ppm/℃(10Ω~10MΩ) ±400ppm/℃(2Ω~10Ω) | ±100ppm/℃(10Ω~1MΩ) ±200ppm/℃(1Ω~10Ω>1MΩ) | ±100ppm/℃(10Ω~1MΩ) ±200ppm/℃(1Ω~10Ω>1MΩ) |

| Type | RC1206 1/4 w | RC1210 1/4 w | RC2010 3/4 w | RC2512 1w |
| --- | --- | --- | --- | --- |
| Operating Temp. Range | －55℃ ~ ＋125℃ |  |
| Maximum Working Voltage | 200V | 200V | 200V | 200V |
| Maximum Overload Voltage | 400V | 400V | 400V | 400V |
| Dielectric Withstanding Voltage | 500V | 500V | 500V | 500V |
| Resistance Range | 1Ω~22MΩ(E-24) 10Ω~2.2MΩ(E-96) Zero Ohm Jumper<0.05Ω | 1Ω~22MΩ(E-24) 10Ω~2.2MΩ(E-96) Zero Ohm Jumper<0.05Ω | 1Ω~22MΩ(E-24) 10Ω~2.2MΩ(E-96) Zero Ohm Jumper<0.05Ω | 1Ω~22MΩ(E-24) 10Ω~2.2MΩ(E-96) Zero Ohm Jumper<0.05Ω |
| Temperature Coefficient | ±100ppm/℃(10Ω~1MΩ) ±200ppm/℃(1Ω~10Ω>1MΩ) | ±100ppm/℃(10Ω~1MΩ) ±200ppm/℃(1Ω~10Ω>1MΩ) | ±100ppm/℃(10Ω~1MΩ) ±200ppm/℃(1Ω~10Ω>1MΩ) | ±100ppm/℃(10Ω~1MΩ) ±200ppm/℃(1Ω~10Ω>1MΩ) |

6. DIMENSIONS                         7. CONSTRUCTION

Unit: mm

| Type | L | W | H | I1 | I2 |
| --- | --- | --- | --- | --- | --- |
| RC0201 | 0.60±0.10 | 0.30±0.05 | 0.25±0.05 | 0.15±0.10 | 0.15±0.10 |
| RC0402 | 1.00±0.10 | 0.50±0.05 | 0.35±0.05 | 0.20±0.10 | 0.25±0.10 |
| RC0603 | 1.60±0.10 | 0.80±0.10 | 0.45±0.10 | 0.25±0.15 | 0.25±0.15 |
| RC0805 | 2.00±0.10 | 1.25±0.10 | 0.50±0.10 | 0.35±0.20 | 0.35±0.20 |
| RC1206 | 3.10±0.10 | 1.60±0.10 | 0.55±0.10 | 0.45±0.20 | 0.40±0.20 |
| RC1210 | 3.10±0.10 | 2.60±0.15 | 0.55±0.10 | 0.50±0.20 | 0.50±0.20 |
| RC2010 | 5.00±0.10 | 2.50±0.15 | 0.55±0.10 | 0.60±0.20 | 0.50±0.20 |
| RC2512 | 6.35±0.10 | 3.20±0.15 | 0.55±0.10 | 0.60±0.20 | 0.50±0.20 |

8. ENVIRONMENTAL CHARACTERISTICS

(1) Temperature Coefficient of Resistance (T.C.R.)

Test Method: Measure resistance at ＋25℃ or specified room temperature as R1, then measure at －55℃ or ＋125℃ respectively as R2.

Determine the temperature coefficient of resistance from the following formula.

R2－R1                             `

T.C.R.＝ ------------  X 106(PPM/℃)

R1 (t2－t1)

Where  t1＝＋25℃ or specified room temperature

t2＝－55℃ or ＋125℃ test temperature

R1＝resistance at reference temperature in ohms.

R2＝resistance at test temperature in ohms.

Acceptance Standard: (Refer to item 5)

- Thermal Shock

Test Method：－55±3℃, 2 minutes and ＋125±2℃, 2 minutes as one cycle. After 5 cycles, the specimen shall be stabilized at room temp. for 1 hour minimum and then measure the resistance to determine △R/R(%).

Acceptance Standard：±(0.5%＋0.05Ω)  for 1% tol.

±(1%＋0.05Ω)   for 5% tol.

(3) Low Temperature Operation

Test Method：Place the specimen in a test chamber maintained at －65  ℃. After one hour stabilization at this temperature, full rated working voltage shall be applied 45  minutes. Have15  minutes after remove the voltage, the specimen shall be removed from the chamber and stabilized at room temperature for 24 hrs.

Measure the resistance to determine △R/R(%).

Acceptance Standard: ±(0.5%＋0.05Ω)  for 1% tol .

±(1.0%＋0.05Ω)  for 5% tol.

& No visible damage

(4) Short Time Overload

Test Method：Apply 2.5 times of rated voltage but not exceeding the maximum overload voltage for 5 seconds. Have the specimen stabilized at room temperature for 30 minutes minimum.

Measure the resistance to determine △R/R(%).

Acceptance Standard: ±(1.0%＋0.05Ω)  for 1% tol.

±(2.0%＋0.05Ω)  for 5% tol.

& No visible damage

(5) Insulation Resistance

Test Method: Place the specimen in the jig and apply a rated continues overload voltage (R.C.O.V) for one minute as shown.

Measure the insulation resistance.

| Type | 0201 | 0402 | 0603 | 0805 | 1206 | 1210 | 2010 | 2512 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Voltage | 50V | 100V | 100V | 300V | 500V | 500V | 500V | 500V |

Acceptance Standard：≧10000MΩ

(6) Dielectric Withstand Voltage

Test Method：Place the specimen in the jig and apply a specified value  continuous overload voltage as shown for one minute.

| Type | 0201 | 0402 | 0603 | 0805 | 1206 | 1210 | 2010 | 2512 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Voltage | 50V | 100V | 100V | 300V | 500V | 500V | 500V | 500V |

Acceptance Standard：Breakdown voltage＞specification and without open/short

(7) Resistance to Soldering Heat

Test Method：Immerse the specimen in the solder pot at 260±5℃

for 10±1 seconds. Have the specimen stabilized at room temperature for 30 minutes minimum.

Measure the resistance to determine △R/R(%).

Acceptance Standard：±(0.5%＋0.05Ω)  for 1% tol.

±(1.0%＋0.05Ω)  for 5% tol.

& No visible damage

(8) Moisture Resistance

Test Method：Place the specimen in the test chamber, and subjected to 42 damp heat cycles. Each one of which consists of the steps 1 to 7 as figure 1. The total length of test is 1000 hours. After the test, have the specimen stabilized at room temperature for 24 hours and measure the resistance to determine △R/R(%).

Acceptance Standard：±(0.5%＋0.05Ω)  for 1% tol.

±(2.0%＋0.05Ω)  for 5% tol.

& no visible damage

Fig. 1   Conditions of change of temperature

(9) Life

Test Method：Place the specimen in the oven at 70±2℃. Apply the rated voltage to the specimen at the 1.5 hours on and 0.5 hour off cycle. The total length of test is 1000 hours. After the test, have the specimen stabilized at room temperature for one hour minimum and measure the △R/R(%).

Acceptance Standard：±(1%＋0.05Ω)  for 1% tol

±(3%＋0.05Ω)  for 5% tol

& no visible damage

(10) Solderability

Test Method：Immerse the specimen in the solder pot at 230±5℃ for 5 sec.

Acceptance Standard：At least 95% solder coverage on the termination.

(11) Bending Strength

Test Method：Mount the specimen on a test board as shown in the figure. Slowly apply the force till the board is bent to specified for

5±1sec,and measure the △R/R(%) at this position.

Acceptance Standard:±(1.0%＋0.05Ω)  for 1% tol.

±(1.0%＋0.05Ω)  for 5% tol.

& No visible damage

| Type | 0201 | 0402 | 0603 | 0805 | 1206 | 1210 | 2010 | 2512 |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Bent distance (d) | 3mm | 3mm | 5mm | 5mm | 5mm | 2mm | 2mm | 2mm |

Unit: mm

(12) Humidity (steady state)

英文參考資料：

Humidity (Steady State)

Test Method：The specimen shall be condition in a dry oven at TEMP. of 40±5℃

for a period of 24 Hr. The specimen shall be placed in a chamber and subjected to

a relative humidity of 90 to 95 percent and a temperature of  40℃±2℃  for the

length of time Hr. When length time subjected to a voltage cycle consisting

of rated  d.c. Voltage application of 1h 30 min and rest of 30 min repeatedly for

one the test duration’s given in h (42 day). Next, the specimen is taken out

of the test chamber, allowed to stand at room temperature for approximately 24 h,

measured for its resistance values again in accordance with 1-1.  And then the

variation in the resistance values taken before and after this test is calculated.

9. TAPING REEL

Unit：mm

| Style | Packaging | Tape width | (A | (B | (C | W | T |
| --- | --- | --- | --- | --- | --- | --- | --- |
| RC0201/RC0402/0603 0805/1206/1210 | Paper | 8mm | 180+0 -3 | 60+1 -0 | 13.0±0.2 | 9.0±0.3 | 11.4±1 |
| 2010/2512 | Embossed | 12mm | 180+0 -3 | 60+1 -0 | 13.0±0.2 | 13.0±0.3 | 15.4±1 |

10. (a)PAPER TAPING

Unit: mm

| Dimension | A | B | W | E | F | P0 | P1 | P2 | ΦD0 | T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RC 0201 | 0.45±0.1 | 0.75±0.1 | 8.0±0.2 | 1.75±0.1 | 3.5±0.05 | 4.0±0.1 | 2.0±0.05 | 2.0±0.05 | 1.5+0.1 -0 | 0.35±0.10 |
| RC 0402 | 0.65±0.1 | 1.15±0.1 | 8.0±0.2 | 1.75±0.1 | 3.5±0.05 | 4.0±0.1 | 2.0±0.05 | 2.0±0.05 | 1.5+0.1 -0 | 0.53±0.10 |
| RC 0603 | 1.1±0.1 | 1.90±0.1 | 8.0±0.2 | 1.75±0.1 | 3.5±0.05 | 4.0±0.1 | 4.0±0.05 | 2.0±0.05 | 1.5+0.1 -0 | 0.70±0.10 |
| RC 0805 | 1.65±0.1 | 2.40±0.1 | 8.0±0.2 | 1.75±0.1 | 3.5±0.05 | 4.0±0.1 | 4.0±0.05 | 2.0±0.05 | 1.5+0.1 -0 | 0.85±0.10 |
| RC 1206 | 1.90±0.1 | 3.50±0.1 | 8.0±0.2 | 1.75±0.1 | 3.5±0.05 | 4.0±0.1 | 4.0±0.05 | 2.0±0.05 | 1.5+0.1 -0 | 0.85±0.10 |
| RC 1210 | 2.80±0.1 | 3.50±0.1 | 8.0±0.2 | 1.75±0.1 | 3.5±0.05 | 4.0±0.1 | 4.0±0.05 | 2.0±0.05 | 1.5+0.1 -0 | 0.85±0.10 |

(b)EMBOSSED TAPING

`

Unit: mm

| Dimension | A | B | W | E | F | P0 | P1 | P2 | ΦD0 | ΦD0 | T |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| RC 2010 | 2.8±0.2 | 5.4±0.2 | 12±0.3 | 1.75±0.1 | 5.5±0.05 | 4.0±0.1 | 4.0±0.01 | 2.0±0.05 | 1.5±0.1 | 1.5±0.25 | 1.0±0.10 |
| RC 2512 | 3.5±0.2 | 6.7±0.2 | 12±0.3 | 1.75±0.1 | 5.5±0.05 | 4.0±0.1 | 4.0±0.01 | 2.0±0.05 | 1.5±0.1 | 1.5±0.25 | 1.0±0.10 |

11. PACKING METHODS

PAPER CARRIER                       EMBOSSED CARRIER

BULK CASSETTE

| Packing Style | Paper Taping Reel (R) | Embossed Taping Reel(K) | Bulk Cassette(C) |
| --- | --- | --- | --- |
|  | 7" (178mm) | 10" (254mm) | 13" (330mm) | 7" (178mm) |  |
| RC0201 | 10,000 | 20,000 | 40,000 | -- | 50,000 |
| RC0402 | 10,000 | 20,000 | 40,000 | -- | 50,000 |
| RC0603 | 5,000 | 10,000 | 20,000 | -- | 25,000 |
| RC0805 | 5,000 | 10,000 | 20,000 | -- | 10,000 |
| RC1206 | 5,000 | 10,000 | 20,000 | -- | -- |
| RC1210 | 5,000 | 10,000 | 20,000 | -- | -- |
| RC2010 | -- | -- | -- | 4,000 | -- |
| RC2512 | -- | -- | -- | 4,000 | -- |

# Text boxes

+5

-0

+5

-0

+0

-5